|  | Roofing Systems |
| --- | --- |

SECTION 07 54 00

THERMOPLASTIC MEMBRANE ROOFING

** NOTE TO SPECIFIER ** Flex Roofing Systems; thermoplastic membrane roofing.
 .
 This section is based on the products of Flex Roofing Systems, which is located at:
5103A Pottsville Pike
Reading, PA 19605
Toll Free Tel: 800-969-0108 
Tel: 610-916-9500
Email: request info (technical@flexmembranes.com)
Web: www.flexroofingsystems.com 
[ Click Here ] for additional information.
 
 Flex Roofing Systems (Flex) is the manufacturer of high quality Thermoplastic Single Ply   PVC (polyvinyl chloride) roof membranes and waterproofing membranes.  Flex Deck is a waterproof traffic membrane manufactured to solve waterproofing problems on various applications, residential, commercial and industrial facilities. Flex Deck is suitable for a waterproofing membrane over a wide range of horizontal substrates and is approved for pedestrian traffic only.
   
 Flex pre-formed flashings, including pipe flanges, inside and outside corners help reduce installation time for penetrations, and corners. 
 Flex provides a complete line of environmentally friendly adhesives for use with thermoplastic single ply roofing membranes.   
 Flex supplies all the metal components required for an outstanding installation, including a full range of fasteners, termination bars, coping cap, gravel stops, fascia, retrofit roof drains, Flexclad metal and accessories.   
 
 Warranty:  Flex Deck Waterproofing systems carry ten year material warranties, depending upon the product used, the method of application, the type of application and the climatic environment.

- GENERAL

  - SECTION INCLUDES

** NOTE TO SPECIFIER **  Delete items below not required for project.

    - Traffic membrane, consisting of welded seam PVC roofing membrane, over the following surfaces as indicated on the Drawings:

      - Balconies, sundecks and roof decks.

      - Walkways and stairways.

      - Patios and courtyards.

      - Swimming pool and hot tub decks.

  - RELATED SECTIONS

** NOTE TO SPECIFIER **  Delete any sections below not relevant to this project; add others as required.

    - Section 07620 - Sheet Metal Flashing and Trim.

    - Section 07500 - Membrane Roofing.

    - Section 07710 - Manufactured Roof Specialties.

    - Section 15160 - Roof Drains.

  - REFERENCES

** NOTE TO SPECIFIER **  Delete references from the list below that are not actually required by the text of the edited section.

    - American Society of Civil Engineers (ASCE) 7 Minimum Design of Loads for Buildings and Other Structures.

    - American Society for Testing and Materials (ASTM) D 1079 - Standard Terminology Relating to Roofing, Waterproofing, and Bituminous Material.

    - American Society for Testing and Materials (ASTM) D 4263 - Standard Test Method for Indicating Moisture in Concrete.

    - American Society for Testing and Materials (ASTM) D 4434 - Standard Specification for Poly (vinyl chloride) Sheet Roofing.

    - National Roofing Contractors Association (NRCA).

    - Sheet Metal and Air Conditioning Contactors National Association, Inc. (SMACNA) Architectural Sheet.

    - Underwriters Laboratories (UL) - Roofing Systems and Materials Guide (TGFU R1306).

  - SUBMITTALS

    - Submit under provisions of Section 01 30 00.

    - Product Data:  Manufacturer's data sheets on each product to be used, including:

      - Preparation instructions and recommendations.

      - Storage and handling requirements and recommendations.

      - Installation methods.

    - Shop Drawings: Installation and seaming plan, showing joints, termination details, and interface with other materials.

    - Selection Samples:  For each finish product specified, two complete sets of color chips representing manufacturer's full range of available colors and patterns.

    - Verification Samples:  For each finish product specified, two samples, minimum size 6 inches (150 mm) square, representing actual product, color, and patterns.

    - Manufacturer's Certificates: Certify products meet or exceed specified requirements

  - QUALITY ASSURANCE

    - Manufacturer Qualifications:

      - Membrane manufacturer shall have a minimum of twenty-five (25) years experience in the production of thermoplastic scrim-reinforced membrane and related accessories.

    - Installer Qualifications:

      - Installer shall have a minimum of five (5) years experience in the application of thermoplastic membrane and shall be certified by the manufacturer of the membrane system.

    - Product Requirements:

** NOTE TO SPECIFIER **  Delete if not required.

      - Membrane Qualifications: Membrane shall be factory certified, first run material, seconds will not be permitted. Approvals:

** NOTE TO SPECIFIER **  Delete requirements not required.

      - The roofing systems shall meet the Underwriters Laboratories Class A requirements.

    - Pre-Installation Conference:

      - Prior to scheduled commencement of the waterproofing installation and associated work conduct a meeting at the project site with the Installer, Architect, Building Owner, Manufacturer's Representative and any other entities directly involved with the performance of the work.

      - The installer shall record conference discussions to include decisions, agreements, and open issues and furnish copies of recorded discussions to each attending party. The primary purpose of the meeting is to review foreseeable methods and procedures related to roofing work schedule and quality.

** NOTE TO SPECIFIER **  Include a mock-up if the project size and/or quality warrant taking such a precaution.  The following is one example of how a mock-up on a large project might be specified.  When deciding on the extent of the mock-up, consider all the major different types of work on the project.

    - Mock-Up:  Provide a mock-up for evaluation of surface preparation techniques and application workmanship.

      - Finish areas designated by Architect.

      - Do not proceed with remaining work until workmanship, color, and sheen are approved by Architect.

      - Refinish mock-up area as required to produce acceptable work.

  - DELIVERY, STORAGE, AND HANDLING

    - Store products in manufacturer's unopened packaging until ready for installation.

    - Protect stored materials from exposure to harmful weather conditions and at temperature and humidity conditions recommended by manufacturer. Leave product wrapped and protected in original packaging with identification labels, until ready for use on the job.

    - Store in a clean, dry, well ventilated area protected from weather and other trades. All rolls of membrane shall be stored, lying down, elevated above the roof deck and completely protected from moisture with tarpaulins.

    - Keep materials at temperature between 40 degrees F (4.4 degrees C) and 80 degrees F (26.6 degrees C); if adhesives are exposed to lower temperature, verify useability with manufacturer before using

    - Store and dispose of solvent-based materials, and materials used with solvent-based materials, in accordance with requirements of local authorities having jurisdiction.

  - PROJECT CONDITIONS

    - Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results.  Do not install products under environmental conditions outside manufacturer's absolute limits.

    - Weather:

      - Proceed with the roof installation only when existing and forecasted weather conditions permit.

      - Ambient Temperatures shall be above 45 degrees F (7 degrees C) when applying water based adhesives or urethane adhesives.

  - WARRANTY

    - Manufacturer warrants to the Building Owner, subject to the terms, limitations, and conditions for a period specified, in which the Materials and Workmanship Warranty is effective, the materials installed shall be free from defects in materials supplied and/or defective workmanship provided by the authorized applicator.

    - Provide manufacturer's 10 or 15-year warranty for membrane leaks due to a manufacturing defect covering waterproofing materials.

.

- PRODUCTS

  - MANUFACTURERS

    - Acceptable Manufacturer: Flex Membrane International Corp., which is located at: 5103A Pottsville Pike, Reading, PA 19605  Toll Free Tel: 800-969-0108 ; Tel: 610-916-9500; Email: request info (technical@flexmembranes.com); Web: www.flexroofingsystems.com

** NOTE TO SPECIFIER **  Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

    - Substitutions:  Not permitted without prior written approval.

    - Requests for substitutions will be considered in accordance with provisions of Section 01 60 00.

  - MATERIALS

- Traffic Membrane: Flex Deck; polyester reinforced PVC membrane chemically formulated to be UV stable and able to resist degradation from the sun. Flex Deck is chemically resistant, stain resistant and has anti-slip properties.	      1. Sheet Width: 76 inches (1930.4mm).

2. Overall Sheet Thickness: 0.060 inch (1.5 mm).

B.	Colors:  Slate Black, Beige, Green

** NOTE TO SPECIFIER **  Delete if not required.

    - Adhesives:

** NOTE TO SPECIFIER **  Delete adhesive not required.

Flex Deck Adhesive: as supplied by Flex Roofing System for laminating membrane to horizontal and vertical surfaces.

      - .

    - B.	Fasteners:

** NOTE TO SPECIFIER **  Delete if not required.

      - Plywood Decks: screw type fasteners applied in a Factory Mutual approved pattern and method.

        - Flex Screws, Corrosion Resistant # 10 Coating

        - SFS Intec Inc., Dekfast Fastening System, C-2 type, corrosion resistant only.

        - OMG Inc.  Fasteners, screws long and short, Endurion coated only.

** NOTE TO SPECIFIER **  Delete if not required.

      - Solid Wood Decks: screw or nail type fasteners:

        - Flex Screws, Corrosion Resistant # 10 Coating

        - SFS Intec, Dekfast Fastening System, C-2 type, corrosion resistant only.

        - OMG Inc., Fasteners, screws long and short, Endurion coated only.

** NOTE TO SPECIFIER **  Delete if not required.

      - Masonry Decks: solid limestone concrete block minimum pullout resistance shall be 525 lb (236 kg), expanded slag block minimum pullout resistance shall be 1100 lb (495 kg), poured concrete, minimum pullout resistance shall be 1000 lb (450 kg):

        - SFS Intec. Dekspike Concrete Roofing Anchor

        - OMG Inc., Fluted Nail or Olympic CD-10

** NOTE TO SPECIFIER **  Delete if not required.

      - C.     Sealants:

1.	Caulking: Silicon, polysulfide or polyurethane caulking, exterior grade for

caulking, surface reglets and vent pipe details.

2.	Mameco, Vulkem 116, Polyurethane.

- Sonneborn, NP1.

4.	BOSTIK, Chem Caulk

5.	For filling pitch pans: Flex Pourable Sealer or as approved by Flex Technical

Services Department.

6. 	Geocel 3300 Polyurethane

    - Flashing:

      - Same material, color and thickness as deck membrane for all curbs,

walls and penetrations.

    - Wood: Nailers.

Number 2 grade lumber  treated for rot and fire resistance.

    - Edge Termination:

      - Size and profile as indicated on drawings.

      - Profiles and designs engineered for roof perimeter attachment.

H. 		Detailing Components

      - Flex Preformed Inside and Outside corners.

      - Flex Split Pipe Boots.

      - Flex Termination Bar.

      - Flex Standard Screws.

      - Flex HD Standard Screws.

- EXECUTION

  - EXAMINATION

    - Do not begin installation until substrates have been properly prepared.

    - If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

    - Verify that deck is:

** NOTE TO SPECIFIER ** Architect must verify the adequacy of the structural support including dead and potential live loads for all surfaces to receive membrane.

      - Secure, well supported, solid, and in accordance with local code structural requirements.

** NOTE TO SPECIFIER ** Minimum required slope is 1 in 100, or 1/8 inch per foot, with an optimum of 1 in 50. 1 in 50 slope, or 1/4 inch in 12 inches, is recommended for all new construction. Coordinate with Drawings to verify proper slopes. For existing construction coordinate details with manufacturer.

      - Properly sloped to drains, valleys, or eaves.

      - Clean and smooth, free of depressions, waves, and projections.

      - Dry and free of ice and snow.

  - PREPARATION

    - Clean surfaces thoroughly prior to installation.

    - Coordinate timing of installation to avoid construction traffic over completed traffic membrane surfaces.

** NOTE TO SPECIFIER ** If wood deck is to be the substrate, delete one of the following two paragraphs. The first is for wood deck without any overlay - combustible. The second is for a non-combustible application. The minimum wood deck that is acceptable is 5/8 inch thick exterior plywood, CDX grade, with tongue-and-groove edges.

    - Wood Deck: Fill joints, knot holes, voids, and low areas with filler and sand smooth.

    - Wood Deck: Cover with cementitious board meeting requirements of Class A approved application. Fill joints, knot holes, voids, and low areas with filler and sand smooth.

** NOTE TO SPECIFIER ** Concrete deck shall be fully cured and have a steel troweled finish.

    - Concrete Deck: Fill surface imperfections and variations with leveling compound.             Test for and remove surface contaminants.

    - Coordinate installation with installation of drains and similar accessories.

    - Install flashings and accessories. Seal around all penetrations, drains, and edges.

    - Membrane shall not come in contact with bituminous materials or polystyrene   insulations. Contact manufacturer for additional information.

    - Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

  - INSTALLATION

    - Install roof system in accordance with manufacturer's instructions applicable codes.

    - Do not install when temperature is below 25 degrees F (minus 3.8 degrees C) or above 98 degrees F (36.6 degrees C). Do not install when winds are gusting over 30 mph (48.3 kph).

    - Do not dilute primers, adhesives, coatings, or sealants.

    - Install membrane with minimum number of seams possible. Overlap seams 3/4 inch (19 mm), to shed water; heat-weld all seams.

    - Adhere membrane to substrate.

    - Mechanically fasten all perimeter edges and penetrations.

  - CLEANING

    - Clean soiled areas in accordance with manufacturer's recommendations.

  - PROTECTION

    - Protect installed products until completion of project.

    - Avoid construction traffic over completed traffic membrane surfaces.

    - Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION